Supplementary information for Monolithic back-end-of-line integration of phase change materials into foundry-manufactured silicon photonics

Maoliang Wei1,†, Kai Xu1,†, Bo Tang2,†, Junying Li1,3,*, Yiting Yun1, Peng Zhang2, Yingchun Wu4,5 Kangjian Bao4,5, Kunhao Lei1, Zequn Chen4,5, Hui Ma1, Chunlei Sun4,5, Ruonan Liu2, Ming Li6,*, Lan Li4,5,*, Hongtao Lin1,*

1 The State Key Lab of Brain-Machine Intelligence, Key Laboratory of Micro-Nano Electronics and Smart System of Zhejiang Province, College of Information Science and Electronic Engineering, Zhejiang University, Hangzhou 310027, China

2 Institute of Microelectronics of the Chinese Academy of Sciences, Beijing 100029, China

3 Hangzhou Institute for Advanced Study, University of Chinese Academy of Sciences, Hangzhou 310024, China

4 Key Laboratory of 3D Micro/Nano Fabrication and Characterization of Zhejiang Province, School of Engineering, Westlake University, Hangzhou, Zhejiang 310030, China

5 Institute of Advanced Technology, Westlake Institute for Advanced Study, Hangzhou, Zhejiang 310024, China

6 State Key Laboratory on Integrated Optoelectronics, Institute of Semiconductors, Chinese Academy of Sciences, Beijing 100083, China

† These authors contributed equally to this work.

* Corresponding author: junyingli@zju.edu.cn; ml@semi.ac.cn; lilan@westlake.edu.cn; hometown@zju.edu.cn

SI.1: Performance of the push-pull MZI modulator with the trimming unit

Fig. S1 Optical and electrical performance of the push-pull MZI modulator with the trimming unit. (a) Measured spectra in the bar and cross states before trimming. (b) Measured current-voltage (I-V) curves before and after the trimming process. (c) Measured dynamic response after the trimming process. (d) Measured O-V curves after applying a 1 MHz radio frequency (RF) signal that lasted for 15 minutes. The performance of the device remains stable after the dynamic response measurement. (e) Spectra measured after the RF signal applied. (f) Spectra measured after 12 days, indicating that the post-trimming possesses good stability and a long retention time.

SI.2: Insertion loss of the Sb2Se3/PIN-doped-Si hybrid waveguide

Fig. S2 Loss of the fabricated Sb2Se3/Si hybrid waveguide. (a) Measured spectra for different numbers of cascaded devices. (b) Extracted loss and linear fit result, indicating that the loss of each Sb2Se3/Si patch is 0.459 dB. The error bars corresponding to the standard deviation of multiple loss characterization results.

SI.3: Push-pull MZI switch without Sb2Se3-assisted trimming

Fig. S3 Performance of the push-pull MZI modulator without Sb2Se3 deposition. (a) Measured O-V curves. The extinction ratio is 18.7 dB (24.5 dB) for the bar (cross) state. (b) Measured spectra at zero bias. (c) Measured spectra of the MZI modulator revealing an insertion loss of 2.31 dB/2.10 dB in the bar/cross state.

SI.4: Simulated loss due to mode mismatch

Fig. S4 Simulated loss originating from the mode mismatch at the interface between an Sb2Se3/Si hybrid waveguide and a silicon waveguide. (a) Simulated mode-mismatch-induced loss in a back-end integrated Sb2Se3/Si hybrid waveguide. (b) Simulated loss of a typical Sb2Se3/Si hybrid waveguide. The simulation indicates that the optical loss is mainly due to mode mismatch instead of the SiO2 trench on the waveguide.

SI.5: Measured quasi-continuous crystallization process of the Sb2Se3-assisted MRR switch.

Fig. S5 (a) Measured quasi-continuous crystallization of the phase-modulated MRR switch. The transmittance change (ΔT) was measured at 1551.513 nm.