## Slide 1: 以非週期性晶疇極化反轉鈮酸鋰達成連續式或主動式Q-調制雙波長Nd:YVO4雷射電光選頻之研究 Electro-optically laser line switchable in a dual-wavelength cw/Q-switched Nd:YVO4 laser based on aperiodically poled lithium niobate
Nonlinear Integrated Laser Photonics (NILP),
Department of Optics and Photonics,
National Central University, Jhongli 320, Taiwan
呂其孟
Chi Meng Lu
指導教授：陳彥宏 博士

## Slide 2
Introduction
  Motivation
  Objective
Working principles
  Gain medium：
  Electro-Optic Effect
  Q-switching
  SFG
Device Design and Simulation Results
  Simulated Annealing Method
  Dual-wavelength Electro-Optic polarization rotation
  Simulation Results
Device Fabrication
  Fabrication process of EO APPLN
Experimental Setup and Results Analysis
  Single pass measurement
  CW operation
  Q-switched operation
Conclusions and Future work
Outline

## Slide 3
Outline
Introduction
  Motivation
  Objective

## Slide 4
Motivation
Applications
Tunable alternate Dual-wavelength for differential absorption lidar (DIAL) systems
Dual-wavelength Raman lidar
Mattis, Ina, et al. Geophysical Research Letters 29.9, P.20-1 (2002)
Dai Hung, Nguyen, and P. Brechignac. Applied optics 27.10, P.1906-1908 (1988)
http://picosure.line88.tw/2018/
http://www.belovedorange.com/
Biomedical Technology using coherent yellow/orange sources
Notes: 1.本實驗可用於雷達技術，雷達技術可被用於測量大氣中的氣態汙染物、氣象參數或化學物種…等等，而本實驗可被作為一個可分別選擇雙波長或不同單一波長的雷達接收器或發射器。
2.橘黃光雷射在生醫、天文觀測、軍事…等受到廣泛的應用，以生醫為例，血紅素對於橘黃光的波段光源有著高度的吸收，可利於外科手術的應用。

## Slide 5
Motivation
CW Lasers
Switchable Multiwavelength Erbium-Doped Fiber Ring Laser With a Multisection High-Birefringence Fiber Loop Mirror
Hu, S., et al. IEEE photonics technology letters 17.7, P.1387-1389, (2005)
Switchable and tunable dual-wavelength erbium-doped fiber laser based on one fiber Bragg grating
Feng, Xinhuan, et al. Optical Fiber Technology 10.3, P.275-282 (2004)
Notes: 1.摻鉺光纖通過單光纖布拉格光柵（FBG），並用單光纖布拉格光柵（FBG）進行橫向應變引起兩個波長之間的間隔，並通過調整偏振控制器（PC）讓雷射可以在兩個波長之間切換
2.摻鉺光纖通過三個不同的FBG得到三個波段的光源，通過高雙折射光纖環鏡並搭配兩個偏振控制器來實現三波長隨機組合切換

## Slide 6
Motivation
CW Lasers
Electro-optic Bragg device and a wavelength selection method utilizing the same
Arie, Ady, and Amir Burstein, U.S. Patent No. 6,584,260. 24 Jun, (2003)
Notes: 1.Arie等人輸入一broadband spectrume光源，我們知道布拉格角度對波長有著很強的依賴性，所以利用不同的角度入射得到不同波長光，入射至電光布拉格繞射元件，並用繞射來達到選頻的作用。
波長與波長的切換時間過長，可能造成系統的不必要的損耗………….

## Slide 7
Motivation
Q-switch Lasers
Actively Q-switched Nd:YVO4 laser using an electro-optic periodically poled lithium niobate crystal as a laser Q-switch
Chen, Y. H., and Y. C. Huang, Optics letters 28.16, p. 1460-1462, (2003)
Theoretical study of the electro-optic effect of aperiodically poled lithium niobate in a Q-switched dual-wavelength laser
Ji, Feng, et al, Optics communications 262.2, p. 234-237, (2006)
Notes: 1.陳彥宏博士等人首次成功的用一塊操作波長為1064nm週期性極化反轉鈮酸鋰晶體並利用電光偏振調制在特定的電場之間快速的切換來達到1064nm的脈衝雷射輸出。
2.延續著陳彥宏博士努力的研究，這群研究者用一塊操作波長在1064nm&1342nm的非週期性鈮酸鋰晶體並利用電光偏振調制在特定的電場之間快速的切換來達到雙波長同時輸出的脈衝雷射光輸出。

## Slide 8
Motivation
Q-switch Lasers
Pulsed orange generation optimized in a diode-pumped Nd: YVO4 laser using monolithic dual PPLN electro-optic Q switches
Chang, W. K., Y. H. Chen, and J. W. Chang, Optics letters 35.16, p. 2687-2689, (2010)
Notes: 1.本實驗室的張煒堃學長用一塊操作波長分別為1064與1342的串級式PPLN並利用兩段電光偏振調制，來達到分別Q調制1064與1342，最終分別輸出單一1064脈衝雷射與單一1342脈衝雷射光，並且在兩波長同時Q調制清況下利用鈮酸鋰晶體的和頻機制得到了操作波長為593的橘黃光脈衝光

## Slide 9
Research ideas
Aperiodic optical superlattice
Signal：1064nm&1342nm
CW 1064nm
CW 1342nm
CW 1064nm&1342nm
Pulse 1064nm
Pulse 1342nm
Pulse 593nm

## Slide 10
Outline
ii. Working principles
  Gain medium：
  Electro-Optic Effect
  Q-switching
  SFG

## Slide 11
Gain medium：
Mirror 2
EO APPLN(2cm)
Mirror 3
c axis
b axis
a axis
Incident light
Nd:YVO4 (a cut)
808nm pump
-polarization
-polarization
The absorption coefficients of the crystal：
-polarization：
-polarization：
Stimulated-Emission Cross Section：
張專慶，陳永富，「利用緊貼組合Nd:YAG 及Nd:YVO4 晶體 實現高效率雙波長946 nm 及1064 nm 雷射」，國立交通大學，碩士論文，民國101年。
3 mm × 3 mm laser aperture and 7 mm length, a-cut, 0.5-at. % Nd3+ doping concentration.
Higher Gain
Lower Gain
TM
Linear polarized > 237：1
Notes: 光子密度
1064nm會搶到上能階大部分的粒子而增益輸出

## Slide 12
Electro-optic Effect
Impermeability tensor of negative uniaxial crystal
EO coefficient of LiNbO3
Difference of impermeability by apply electric field
Refractive index ellipsoid equation
Electro-optic Effect in LiNbO3
Yariv & Yeh “Optical waves in crystals” chap.7, P.463, (2003)
V
V
Plate
Plate
x
z
y
x
z
y
Notes: 鈮酸鋰為電光晶體，本實驗利用施加Y方向電場的電光效應，鈮酸鋰晶體正晶疇r51為正，光軸旋轉角為負theta，鈮酸鋰晶體負晶疇r51為負，光軸選旋轉角為負theta
1.負單軸晶體不加電場的反介電張量
2.鈮酸鋰晶體電光係數
3.施加電場的反介電張量的變化量

## Slide 13
Electro-optic Effect
Schematic diagram of type filter
；m=1,2,3…
Schematic diagram of type polarization rotating
type filter in PPLN Crystal
V
type filter in LiNbO3
Notes: 索爾克濾波器為兩種不同半波版交疊排列所組成，一種為…，一種為…，而工作原理為…….與原偏振差4theta以此排列下去，最終可將偏振旋轉成水平偏振，所而克濾波器好比於鈮酸李正副晶疇週期排列。

## Slide 14
Q-switching
Fast decay
Ground
808nm Pump
4F3/2
Pump band
1064nm
4F11/2
4F13/2
1342nm
CW Output
Pulse Output
c axis
b axis
a axis
Incident light
a axis
b axis
c axis
Incident light
Nd:YVO4 (a cut)
Nd:YVO4 (c cut)
3 mm × 3 mm laser aperture and 7 mm length, a-cut, 0.5-at. % Nd3+ doping concentration.
Electric field(V/mm)
Transmittance(A.U.)

## Slide 15
SFG
Conservation of momentum
Conservation of energy

## Slide 16
Outline
iii. Device Design and Simulation Results
  Simulated Annealing Method
  Dual-wavelength Electro-Optic polarization rotation
  Simulation Results

## Slide 17
Simulated Annealing Method
Set the initial condition：Domain number=N,
Domain(j), j=0
Set the object Function(OF) Calculation, OF(0)
Set the parameter of annealing：、、
end
Yes
Yes
Yes
No
No
No
No
Yes

## Slide 18
Objective Function
Device design parameters
Crystal length：2cm
Phase matching temperature ：40℃
Signal wavelength：1064nm & 1342nm
Object function target value：
1mm
2cm
Target value
Actual value
Initial value
Initial value
Actual value
Target value
Simulated Annealing Method
Notes: TM偏振穿透率對電場進行SIN波振盪

## Slide 19
Electric field(V/mm)
TM polarization-Transmittance(A.U.)
1064.50nm
1342.33nm
Wavelength(nm)
Transmittance(A.U.)
233V/mm
822V/mm
Device design result
Wavelength(nm)
Transmittance(A.U.)
Wavelength(nm)
Transmittance(A.U.)
Wavelength(nm)
Transmittance(A.U.)
Electric field(V/mm)
TM polarization-Transmittance(A.U.)
1064.50nm
1342.33nm
Simulated Annealing Method

## Slide 20
Round trip calculation
EO APPLN()
Round Trip
EO APPLN()
Round Trip + Single pass
808nm Laser
808nm Laser

## Slide 21
Outline
iv. Device Fabrication
  Fabrication process of EO APPLN

## Slide 22
Fabrication process of EO APPLN
clean wafer
Photoresist coating
Exposure
Development
Soft baking
Hard baking
Schematic diagram of positive photomask
Schematic diagram of chip after lithography

## Slide 23
Poling fixture
Inject in poling fixture
Applied high electric field
after poling and etching
Fabrication process of EO APPLN

## Slide 24
Dicing, Polishing, Coating
Diagram of the EOAPPLN after endface polishing
Polishing
Coating
Completed product
Diagram of the EOAPPLN after coating

## Slide 25
Outline
v. Experimental Setup and Results Analysis
  Single pass measurement
  CW operation
  Q-switched operation

## Slide 26
Single pass measurement
I:7.0A
V:23.2V
T
C
on
Pump laser:
809nm diode laser
Mirror 1
LIMQ laser system
Mirror 2,3
OK
Unit
f=75mm
f=125mm
Iris
PBS
Power meter
HR@808nm filter
Mirror 1: Meniscus mirror; ROC=15 cm T~93%@809 nm, HR~99.8%@1064 nm, HR~99.8%@1342 nm
POWER SUPPLY
EO APPLN()
Plastic screw
Acrylic
Teflon
brass
EO-APPLN()
Heater
Temperature sensor
Mirror 2: Plane mirror; HR~99.908%@1342 nm HT~96.256%@1064nm
Mirror 3: Plane mirror; HR~61.3%@1064 nm HT~99.3%@1342nm
Temperature Controller

## Slide 27
Extra-cavity single pass measurement
Poling error effect
Under-poled
Under-poled
Under-poled
Poling error effect
No poling error
Simulation EO coefficient：
26pm/V
Simulation Temperature：
40℃
Fitting Temperature：
40.2℃
Fitting EO coefficient：
24pm/V
Under-poled：
Single pass measurement

## Slide 28
CW operation
Preset
Power
ANRITSU
MS9740A
Level
Peak
Select
Marker
Marker
Search
Sweep
I:7.0A
V:23.2V
T
C
on
Fiber Coupled
809nm laser diode
Mirror 1
LIMQ laser system
Mirror 1: Meniscus mirror; ROC=15 cm T~93%@809 nm, HR~99.8%@1064 nm, HR~99.8%@1342 nm
Mirror 2: Plane mirror; HR~99.908%@1342 nm HT~96.256%@1064nm
Mirror 3: Plane mirror; HR~61.3%@1064 nm HT~99.3%@1342nm
Mirror 3
HR@808nm filter
7.4cm
12cm
Mirror 2
POWER SUPPLY
EO APPLN(2cm)
OSA

## Slide 29
0V/mm
267V/mm
685V/mm
895V/mm
CW operation

## Slide 30
267V/mm
255V/mm
243V/mm
275V/mm
286V/mm
244V/mm
285V/mm
1064.5nm Tolerance：42V/mm
0.02714
Electric field(V/mm)
TM polarization-Transmittance(A.U.)
1064.50nm
1342.33nm
CW operation

## Slide 31
895V/mm
891V/mm
883V/mm
907V/mm
917V/mm
884V/mm
916V/mm
1342.33nm Tolerance：33V/mm
31
0.04875
Electric field(V/mm)
TM polarization-Transmittance(A.U.)
1064.50nm
1342.33nm
CW operation

## Slide 32
Q-switched operation
I:7.0A
V:23.2V
T
C
on
Fiber Coupled
809nm laser diode
Mirror 1
LIMQ laser system
Mirror 1: Meniscus mirror; ROC=15 cm T~93%@809 nm, HR~99.8%@1064 nm, HR~99.8%@1342 nm
Mirror 2: Plane mirror; HR~99.908%@1342 nm HT~96.256%@1064nm
Mirror 3: Plane mirror; HR~61.3%@1064 nm HT~99.3%@1342nm
Mirror 3
HR@808nm filter
7.4cm
12cm
Mirror 2
EO APPLN(2cm)
1
3
2
4
5
6
8
7
9
0
.
→
←
menu
LOCAL
STOP
ENTER
Oscilloscope
POWER SUPPLY
pulser
CH 1
POWER SUPPLY
1
2
CH 2
Notes: 正行方波電壓脈衝訊號，正端為上升後的電壓，也就是HIGH-Q電壓另一台接負端作為偏壓電源，提申至特定的直流準位，GROUND提升至LOWQ電壓。
負方波電壓脈衝訊號，負端坐為下降後的電壓，也就是HIGH-Q電壓另一台接正端作為偏壓電源，，提申至特定的直流準位，GROUND提升至LOWQ電壓。

## Slide 33
1064nm Pulse width
532nm
532nm Pulse width
685V
267V
685V
261V
685V
269V
685V
255V
685V
273V
pulser
CH 1
1064nm
POWER SUPPLY
POWER SUPPLY
1
2
1064.50nm
1342.33nm
Electric field(V/mm)
Transmittance(A.U.)
Q-switched operation

## Slide 34
POWER SUPPLY
1342nm Pulse width
671nm
671nm Pulse width
POWER SUPPLY
pulser
1
2
1342nm
685V
875V
680V
875V
685V
895V
685V
897V
685V
901V
CH 2
1064.50nm
1342.33nm
Electric field(V/mm)
Transmittance(A.U.)
Q-switched operation

## Slide 35
593nm
593nm Pulse width
pulser
CH 1
POWER SUPPLY
POWER SUPPLY
1
2
685V
0V
685V
0V
685V
2V
685V
0V
685V
3V
1064.50nm
1342.33nm
Electric field(V/mm)
Transmittance(A.U.)
Q-switched operation

## Slide 36
Outline
vi. Conclusions and Future work

## Slide 37
Conclusions
We use the simulated annealing method to calculate an aperiodically poled lithium niobite device for achieving a novel electro-optically laser-line switchable dual-wavelength cw/Q-switched Nd:YVO4 laser
We successfully achieved wavelength selection via EO tuning in a cw dual-wavelength 1064.5nm and 1342.33nm laser with electric field tuning tolerances of ~42V/mm and ~33V/mm, respectively.
When the system is operated at a repetition rate of 1kHz and a pump power of ~7.014W, we can obtain pulsed 1064 nm, 1342 nm, 593 nm orange, 532 nm green, and 671 nm red generations simply by EO tuning:
Wavelength | Pulse width | Peak power | Applied electric field
1064nm | 9.6140ns | 18.5kW | 267V/mm 685V/mm
532nm (non-phase matching) | 8.7368ns | 30.79W | 
1342nm | 25.4740ns | 13.8kW | 685V/mm 895V/mm
671nm (non-phase matching) | 15.0374ns | 9.71W | 
593nm (non-phase matching) | 8.0198ns | 74.19W | 0V/mm 685V/mm
Wavelength | Pulse width | Peak power | Applied electric field
1064nm | 9.6140ns | 18.5kW | 
532nm (non-phase matching) | 8.7368ns | 30.79W | 
1342nm | 25.4740ns | 13.8kW | 
671nm (non-phase matching) | 15.0374ns | 9.71W | 
593nm (non-phase matching) | 8.0198ns | 74.19W | 

## Slide 38
Future work
b axis
a axis
Incident light
Nd:YLF (a cut)
c axis
1047nm
1053nm
6nm
Wavelength(nm)
Transmittance(A.U.)
Wavelength(nm)
Transmittance(A.U.)
Wavelength(nm)
Transmittance(A.U.)
Wavelength(nm)
Transmittance(A.U.)
230V/mm
372V/mm
1047nm
1053nm
Electric field(V/mm)
Transmittance(A.U.)
李瑋倫、陳永富，摻釹氟化釔鋰晶體在連續波與被動式 Q 開關雷射之研究。Diss, (2010)

## Slide 39
Thank you for your attention!

## Slide 40
16A
17A
18A
19A
20A
1064.549nm
1064.518nm
1064.547nm
1064.539nm
1064.529nm
16A
17A
18A
19A
20A
0.031nm

## Slide 41
1064.500nm
1064.469nm
0.031nm
Electric field(V/mm)
TM polarization-Transmittance(A.U.)
1064.500nm
1342.33nm
1064.469nm

## Slide 42
Mirror 1
Mirror 2
Mirror 1
Mirror 2
Loss↑