## Slide 1: Nonperiodic optical superlattice lithium niobite waveguides for the generation of polarization entanglement
Wen-Chiuan Su1, Jasleen Lugani2, Frank Setzpfandt2, and Yen-Hung Chen1
1Department of Optics and Photonics, National Central University, Taiwan (R.O.C.)
2Institute of Applied Physics, Friedrich-Schiller-University Jena, Germany
Acknowledgement
This work was supported by the Ministry of Science and Technology of Taiwan (MOST)
Notes: Good afternoon everyone. I’m Wen-Chiuan Su from National Central University in Taiwan. Today I’m going to talk about ‘’.

## Slide 2: Outline
Introduction
Working Principle
Simulation
Fabrication
Results
Future Work & Summary
Notes: Here’s the outline. I will talk about why and how we study this topic. Then give the results of simulation, fabrication and measurement.

## Slide 3: Introduction
Phys. Rev. Lett. 59 (17): 1903–1905. (1987).
Phys. Rev. Lett. 25 (2): 84. (1970).
Quantum information
Quantum cryptography
Quantum computation
etc.
J. Opt. Soc. Am. B 21, 2081-2084
Spontaneous Parametric Down-Conversion
SPDC with quantum phenomenon
SPDC in bulk PPKTP
Notes: Let me now just focus on the periodically poled crystal using in SPDC process. In the beginning, many groups are using bulk crystal to generate photon pairs, such as KTP. Then people come up an idea of using waveguide to guide the light into a small area. That can make the efficiency much higher. Then people start to do the research of SPDC in LN waveguide because of some advantages.

## Slide 4: Introduction
SPDC in PPKTP waveguide
Opt. Express 15, 7479-7488 (2007)
New J. Phys. 12 103005
Opt. Express 20, 5508-5517 (2012)
SPDC in cascade PPLN
SPDC in PPLN waveguide
SPDC in dual-periodically-poled structure
Opt. Lett. 44(22), 5598–5601 (2019).
Notes: Let me now just focus on the periodically poled crystal using in SPDC process. In the beginning, many groups are using bulk crystal to generate photon pairs, such as KTP. Then people come up an idea of using waveguide to guide the light into a small area. That can make the efficiency much higher. Then people start to do the research of SPDC in LN waveguide because of some advantages.

## Slide 5: Introduction
In this study
Advantages
Compact
Designable multiple photon pairs
Eliminate time delay
Pump wavelength = 780 nm, TE
Signal wavelength = 1550 nm, TE & TM
Idler wavelength = 1570 nm, TM & TE
Notes: Let me now just focus on the periodically poled crystal using in SPDC process. In the beginning, many groups are using bulk crystal to generate photon pairs, such as KTP. Then people come up an idea of using waveguide to guide the light into a small area. That can make the efficiency much higher. Then people start to do the research of SPDC in LN waveguide because of some advantages.

## Slide 6: Working Principle
Sum Frequency Generation (SFG)
Momentum Conservation (Quasi Phase Matching)
Energy Conservation
Χ(2) crystal
ω3
ω1
ω2

## Slide 7: Working Principle
Spontaneous Parametric Down Conversion (SPDC)
Momentum Conservation (Quasi Phase Matching)
Energy Conservation
Χ(2) crystal
ωp
ωs
ωi
與OPG(Optical parametric generation)的差異 : 操作能量的不同

## Slide 8: Working Principle
Aperiodically Poled Lithium Niobate (APPLN)
↑ | ↓ | ↑ | ↓ | ↑ | ↓ | ↑ | ↓ | ↑ | ↓ | ↑ | ↓ | ↑ | ↓ | ↑ | ↓ | ↑ | ↓ | ↑ | ↓
↑ | ↓ | ↑ | ↓ | ↑ | ↓ | ↑ | ↓ | ↑ | ↓ | ↑ | ↓ | ↑ | ↓
periodically poled
aperiodically poled
Λ
Potential energy
矯頑電場

## Slide 9: Working Principle
Genetic Algorithm (GA)
產生初始個體
交配
達到最佳解
突變
結束
計算適應度
是
否

## Slide 10: Simulation
Genetic Algorithm (GA)
: 空間頻率所對應的傅立葉係數
: 空間頻率所計算出來的傅立葉係數理 論值
: 空間頻率的權重
: 等高權重

## Slide 11: Simulation
Genetic Algorithm (GA)
9.71 μm
9.65 μm

## Slide 12: Fabrication
Waveguide Process
平均距離 = 7.10 μm

## Slide 13: Fabrication
Poling Process

## Slide 14: Results
Setup for Spatial Mode Experiment

## Slide 15: Results
Spatial mode
 | Δn(1550, TM) | Δn(1550, TE) | Depth(μm)
Measurement | 0.00527 | 0.00133 | 8.332
Simulation | 0.01136 | 0.00504 | 

## Slide 16: Results
Setup for SHG Experiment

## Slide 17: Results
Varying Temperature
Wavelength shifting
measurement : -0.23 nm/℃
simulation : -0.25 nm/℃

## Slide 18: Results
Dual Peaks Measurement
220℃
Peak wavelength : 1575.49 nm & 1580.94 nm
Peak differences
measurement : 5.6 nm
simulation : 4.4 nm
Red line : simulation
Blue line : measurement

## Slide 19: Results
Varying Pump Power
First Peak
Second Peak
λ=1575.49 nm
λ=1580.94 nm

## Slide 20: Results
Setup for SFG Experiment

## Slide 21: Results
Setup for SFG Experiment
chip

## Slide 22: Results
Sum Frequency Generation (SFG)
TM
TE
TM
TE
Measurement
(condition 1)
Measurement
(condition 2)
Λ1
Λ1
Λ2
Λ2

## Slide 23: Results
Sum Frequency Generation (SFG)
Measurement (condition 3)
Simulation

## Slide 24: Results
SFG to SPDC Reconstruction
Reconstruction
Simulation
Λ1
Λ2
Λ1
Λ2
TE
TM

## Slide 25: Summary
Photons from different processes can be generated in an aperiodically poled structure.
Wavelength can be tuned by changing temperature.
Predict SPDC spectrum by reconstructing the SFG result.
First to generate multiple photon pairs by using an aperiodically poled structure.

## Slide 26: Future Work
累積的折射率差值
晶體長度
SPDC
Y-field
EOPMC
Z-field
electrode
等長
Time delay
Wavelength shifting
Problems
Solution
Electro-optic Polarization Mode Converter (EOPMC)
SPDC
Electro-optic Polarization Mode Converter
Time compensation
part

## Slide 27: Future Work
Electro-optic Polarization Mode Converter (EOPMC)
Searcy, P., et al., Proceedings of SPIE - The International Society for Optical Engineering, 2010. 7672
Electro-optic coefficient of LiNbO3
applying electric field along Y direction

## Slide 28: Future Work
Electro-optic Polarization Mode Converter (EOPMC)
Bandwidth (T>99%) : 1.71 nm
Bandwidth (T>99%) : 1.58 nm
Applied voltage = 100V

## Slide 30
Thank you for your attention!
Nonlinear Integrated Laser Photonics Lab (NILP)