## Slide 1
以積體鈮酸鋰波導光參量放大器及絕熱耦合分光器達成晶片型量子壓縮光源之研究
On-chip quantum squeezer based on integrated lithium niobate waveguide optical parametric amplifier and adiabatic beam splitter
學生: 高梃澄
指導教授: 陳彥宏 博士
Nonlinear Integrated Laser Photonics Lab (NILP), Department of Optics and Photonics, National Central University, Jhongli 320, Taiwan
Notes: 各位口試委員，午安，大家好，我是高梃澄，今天我要報告的題目是…，

## Slide 2
Introduction
Theory
  Quantum state
  Balance homodyne detection(BHD)
  Sum frequency generation(SFG)/Optical parametric amplifier(OPA)
  Quasi-phase matching(QPM)
  Stimulated Raman adiabatic passage(STIRAP)
Simulation
  Adiabatic beam splitter design
  High-pass filter simulation
Fabrication process
  Ti-indiffused waveguide
  Electric field poling
  End face polish
Experimental Results and Analysis
  Propagation loss
  ER spectrum
  SHG characteristic
  Squeezing light optical setup
Conclusion and future work
Notes: Outline順過
在各部分在介紹為何這樣編排

## Slide 3
Introduction
Roman Schnabel et al, Nature Communications, 1(20210)
Notes: 壓縮光是非古典的光在某個正交項會比一般古典光的雜訊還要低，根據海森堡不確定性原理，相干態的雜訊定義出標準量子雜訊，透過壓縮光特性可以超過這個量子極限，以提高感測上的精準度
a.(i)shot-noise(ii)squeezed noise表示壓縮光的光子數統計下小於shot-noise
b.透過Michelson干涉儀將一般雷射和壓縮光做干涉，能夠提升訊雜比
比較1284Hz調制訊號，沒壓縮光參與看不到訊號，可以在c.光電流圖d.雜訊頻譜圖

## Slide 4
Integrated quantum light source chip, compact and stable:
OPA high bandwidth enhance quantum computation
AC fabrication tolerant and broadband
In CW scheme | OPO(cavity) | OPA(waveguide)
Squeezing level | 15dB[1] | 6dB[2]
Bandwidth | ~GHz | ~THz
volume | large | small
Motivation
Pumping source | Pulse | CW
Squeezing level | large | small
Damage effect | Gain-induced diffraction | Photorefractive
Mode match | Temporal mode mismatching | x
[1]Henning Vahlbruch et al, Phys. Rev. Lett. 117(2016)
[2]Takahiro Kashiwazaki et al, APL Photonics 5, 036104 (2020)
Notes: 進步性跟其他研究

## Slide 5
Chip design
Notes: 晶片是使用type-0 OPA方式將真空態轉成真空壓縮態
後面接一段絕熱耦和分光器將pump 775nm和signal 1550nm分開
完成積體化晶片型量子壓縮光源

## Slide 6
Introduction
Theory
  Quantum state
  Balance homodyne detection(BHD)
  Sum frequency generation(SFG)/Optical parametric amplifier(OPA)
  Quasi-phase matching(QPM)
  Stimulated Raman adiabatic passage(STIRAP)
Simulation
  Adiabatic beam splitter design
  High-pass filter simulation
Fabrication process
  Ti-indiffused waveguide
  Electric field poling
  End face polish
Experimental Results and Analysis
  Propagation loss
  ER spectrum
  SHG characteristic
  Squeezing light optical setup
Conclusion and future work

## Slide 7
Quantum state
Amplitude , Phase
Quadrature operator general form:
D. J. Griffiths and D. F. Schroeter, Introduction to Quantum Mechanics, Third edition ed. Cambridge University Press(2018)
Notes: 量子化光場
正交算符由上升合下降算符表示為
零點能量對應到vacuum state
相位圖、time domain上量測可以看到隨著干涉的相位差改變而出現建設性和破壞性的干涉現象

## Slide 8
Vacuum state
According to Heisenberg uncertainty principle
Amplitude variance , Phase variance
Coherent or vacuum state have minimum uncertainty
Vacuum state
G. L. Mansell,"Squeezed light sources for current and future interferometric gravitational-wave detectors",PhD thesis,Australian National University(2018)
Notes: 量子態中最基本的是真空態
海森堡不確定性原理，得到兩個正交態的變異數的乘積最小為1
振幅和相位皆為1，對應到的正是相干態或是真空態的正交算符變異數如左圖

## Slide 9
Squeezed vacuum state
r : squeezing parameter
: second harmonic efficiency
P : pump power
Squeezed vacuum state
G. L. Mansell,"Squeezed light sources for current and future interferometric gravitational-wave detectors",PhD thesis,Australian National University(2018)
Notes: 從不確定原理中可以預測出是不是有個量子態可以達到在某一個正交態小於1而另一部份大於1，這個量子態就是壓縮態
左圖是真空壓縮態
右邊變異數的成績依舊為1，其中的r 稱作壓縮參數，和倍頻轉換效率、pump能量有關

## Slide 10
Balance homodyne detection(BHD)
is BS transmittance, is amplitude
= 0 → quadrature amplitude operator
= π/2 → quadrature phase operator
Mode match(visibility)
Notes: 量測真空壓縮光的方法是利用干涉的技術將coherent state、squeezed vacuum state干涉，並將兩道干涉光經由光偵測器後相減，稱作BHD
能夠將壓縮光微量的雜訊擾動透過本地振盪器(Local Oscillator)放大
推導中 透過BHD技術可以量測任意的正交項變異數
Visibility描述的是兩道光的重合程度，重合度愈高代表LO可以有效地去放大壓縮光正交算符的變異數並偵測

## Slide 11
Sum frequency generation(SHG)/OPA
Conservation of Energy i.e. frequency-matching condition
Down-conversion
Up-conversion
Correspond to squeezed operator
C. Gerry and P. Knight, Introductory Quantum Optics. Cambridge University Press(2004)
Change the signal photon to vacuum
Notes: 要產生非線性過程需要滿足能量守恆、動量守恆也就是相位匹配會在下一張投影片解釋
上轉換SHG
下轉換OPA
最後想產生真空壓縮態，可以將seed光類比成vacuum達到真空態轉成真空壓縮態

## Slide 12
Quasi-phase matching(QPM)
Use electric poling technology produce periodic inversion domain grating.
Compensated the phase mismatch in waveguides.
O. Alibart et al., "Quantum photonics at telecom wavelengths based on lithium niobate waveguides," Journal of Optics (United Kingdom), vol. 18, no. 10(2016)
Conservation of Momentum i.e. phase-matching condition
Notes: 能夠外加電場讓晶疇反轉，達到相位補償，稱作準相位匹配如左圖
右圖是PPM QPM NPM

## Slide 13
Phase-Matching condition
Key parameter
: phase difference
More nonlinear conversion efficiency parameter
: pump power
: effective nonlinear coefficient
: crystal length
R. W. Boyd, Nonlinear Optics, 4th Edition ed. Academic Press(2020)
Notes: 相位匹配在一般anisotropic晶體因為色散關係無法有相位匹配，本研究所使用的是LN晶體為負單軸雙折射晶體
在和頻實驗中，可以推導出右邊方程式，其中正是影響著整個非線性轉換是否有效率
呼應前面提到的壓縮參數r和非線性轉換效率有關，在方程式中可以看到pump power、等效非線性係數以及晶體的長度，在相同波導結構中控制這三個參數能夠達到最高的轉換效率
左邊為和頻量測的實驗結果
本實驗為了有高非線性轉換效率，使用type-0拿到d33最高的非線性係數做轉換，也就是TM pump轉成TM signal+TM idler。
相位匹配在一般anisotropic晶體因為色散關係無法有相位匹配，本研究所使用的是LN晶體為負單軸雙折射晶體
在和頻實驗中，可以推導出右邊方程式，其中∆𝑘正是影響著整個非線性轉換是否有效率
呼應前面提到的壓縮參數r和非線性轉換效率有關，在方程式中可以看到𝐴_1 𝐴_2pump power、等效非線性係數以及晶體的長度，在相同波導結構中控制這三個參數能夠達到最高的轉換效率
左邊為和頻量測的實驗結果
本實驗為了有高非線性轉換效率，使用type-0拿到d33最高的非線性係數做轉換，也就是TM pump轉成TM signal+TM idler。

## Slide 14
Counter-intuitive ordering
Stimulated Raman adiabatic passage (STIRAP)
Intuitive ordering
In resonance condition(),
Hamiltonian:
T. H. Nikolay et al, "Laser-induced population transfer by adiabatic passage techniques," Annual Review of Physical Chemistry, vol. 52, no. 1, pp. 763-809(2001)
B. W. Shore, "Picturing stimulated Raman adiabatic passage: a STIRAP tutorial," Advances in Optics and Photonics, vol. 9, no. 3(2017)
Notes: STIRAP是透過拉比共振和絕熱過程，利用兩者的優點，使粒子能夠產生了穩定的共振效應，在共振系統中Hamiltonian描述如投影片中的矩陣
三能階系統 粒子數轉換 在時間上是先P再S是拉比共振過程
先P再S可以達到23能階先有相干疊加，後續S進來可以直接將粒子從1轉換3能階，當系統交互作用足夠緩慢，就不會激發2能階，稱作絕熱過程
此時時間上粒子分布和pulses是反直覺的過程
STIRAP是透過拉比共振和絕熱過程，利用兩者的優點，使粒子能夠產生了穩定的共振效應∆_𝑝=∆_𝑠，在共振系統中Hamiltonian描述如投影片中的矩陣
三能階系統 粒子數轉換 在時間上是先P再S是拉比共振過程
先P再S可以達到23能階先有相干疊加，後續S進來可以直接將粒子從1轉換3能階，當系統交互作用足夠緩慢，就不會激發2能階，稱作絕熱過程
此時時間上粒子分布和pulses是反直覺的過程

## Slide 15
Stimulated Raman adiabatic passage (STIRAP)
coupling constant
: coupling length
: adiabatic parameters
r, : fabrication constant
H. P.Chung et al., "Adiabatic light transfer in titanium diffused lithium niobate waveguides," Optics Express, vol. 23, no. 24, p. 30641(2015)
Adiabatic condition：
Finally, adiabatic condition：
Therefore, we design adiabatic beam splitter via , ,
Notes: 將拉比共振換成耦合係數、將時間域換成空間域，同樣在一個三能階系統中
絕熱性是否足夠可以透過絕熱條件來判斷
分子…
分母…
最後調整三個參數
將拉比共振換成耦合係數、將時間域換成空間域，同樣在一個三能階系統中
絕熱性是否足夠可以透過絕熱條件γ來判斷…

## Slide 16
Introduction
Theory
Simulation
  Adiabatic beam splitter design
  High-pass filter simulation
Fabrication process
  Ti-indiffused waveguide
  Electric field poling
  End face polish
Experimental Results and Analysis
  Propagation loss
  ER spectrum
  SHG characteristic
  Squeezing light optical setup
Conclusion and future work

## Slide 17
Second version
Adiabatic beam splitter design
Problems:
First version: use 785nm laser diode observe high-order mode at signal output.
Second version: design another adiabatic coupler to eliminate pump high-order mode at signal output. Due to fabrication limit, need to shorter coupling length cause adiabatically reduced. 1550nm has 5dB coupling efficiency as well as 76% power loss.
Finally, adopt five waveguides array to enhance the effective refractive index too close between pump and signal wavelength.
First version
pump port
signal port
Notes: 中間圖要改 775nm 775高模 右圖要改

## Slide 18
Adiabatic beam splitter design
adiabatic condition：

## Slide 19
High-pass filter simulation
Notes: 1550ER

## Slide 20
(a)1500nm、(b)1550nm、(c)1600nm
High-pass filter simulation BPM(signal)

## Slide 21
High-pass filter simulation

## Slide 22
High-pass filter simulation BPM(pump)
(a)725nm、(b)775nm、(c)825nm

## Slide 23
Introduction
Theory
Simulation
Fabrication process
  Ti-indiffused waveguide
  Electric field poling
  End face polish
Experimental Results and Analysis
  Propagation loss
  ER spectrum
  SHG characteristic
  Squeezing light optical setup
Conclusion and future work
Notes: 首先製作Ti波導
在透過外加電場反轉晶疇 達到週期性結構
最後經過端面處理才能進入量測部分

## Slide 24
Ti-indiffused waveguide-lithography
Waveguides develop figures x10/x100

## Slide 25
Ti-indiffused waveguide-diffusion
x100 waveguides lift-off/indiffused figures

## Slide 26
Electric field poling-lithography
Poling period develop figures x10

## Slide 27
Electric field poling-poled
Poling period etch figures x10/x100

## Slide 28
End face polish-chemical-mechanical polishing
Side view Chip both edges
(a)
(b)
(c)
LN
LN
chip

## Slide 29
Introduction
Theory
Simulation
Fabrication process
Experimental Results and Analysis
  Propagation loss
  ER spectrum
  SHG characteristic
  Squeezing light optical setup
Conclusion and future work

## Slide 30
Beam splitter scheme

## Slide 31
Waveguide TM mode profile
1550nm
775nm

## Slide 32
Waveguide TM mode profile
1540nm
1550nm
Extend the propagation distance for eliminate background noise

## Slide 33
ER spectrum
Notes: ER>10dB with 50nm

## Slide 34
SHG scheme

## Slide 35
SHG spectrum
在40℃下，不同週期的倍頻
在同週期17.21μm下，不同溫度的倍頻結果

## Slide 36
Tuning rate
Estimate the tuning rate 0.134nm/

## Slide 37
Squeezing light scheme

## Slide 38
Real optical setup
Squeezed waveguide couple
LO waveguide couple
Coherent light source
Balance homodyne detection

## Slide 39
Detail setup
LO waveguide coupling
squeezed waveguide coupling
BHD

## Slide 40
Improve visibility
1550nm Waveguide mode profile(a)squeezed arm、(b)LO arm
Optimize mode match efficiency 1.65 times as well as observe squeezing level
fiber() /waveguide mode()

## Slide 41
Spectrum analyzer
Different LO power correspond to shot noise

## Slide 42
775nm waveguide mode profile. Adjust the objective lens focal position to waveguide.
If (a) at Xmm、(b)at X+0.25mm
That is, 0.25mm range can’t deduce which position is the optimized.
Free space coupling efficiency~8.4dB
Improve 775nm coupling loss

## Slide 43
Improve 775nm coupling loss
Fiber coupling efficiency~4.8dB
Optimize pump coupling efficiency 2.29 times in waveguide

## Slide 44
Calculation squeezing level
Zhang, Mi, "Study of Spatial Structure of Squeezed Vacuum Field“, Dissertations(2016)
T. Kashiwazaki et al., "Continuous-wave 6-dB-squeezed light with 2.5-THz-bandwidth from single-mode PPLN waveguide," APL Photonics, vol. 5, no. 3, 2020
: Anti-squeezing level
: Squeezing level
: SH conversion efficiency
: SH conversion efficiency root
: Total effective detection efficiency
r=*= =
= 100 = 100
Use shot noise as a reference

## Slide 45
Calculation squeezing level
 | 2020[11] (PPLN) | 2020[53] (PPLN) | 2019[1] (PPLN+DC) | 2018[4] (PPLN+3*DC) | 2016[12] (PPLN) | Our estimate (PPLN)
Squeezing Level(dB) | -6.3 | -4 | -2 | -1.38 | -1.83 | -0.67
Waveguide type | Ridgea | Ridgeb | SPE | RPE | Ridgec | Ti
QPM length(mm) | 45 | 45 | 30 | 20 | 40 | 15
norm(%/W/cm2) | 57.28 |  |  | 92.5 | 125 | 15.8
) | 0.108 |  |  | 0.061 | 0.141 | 0.019
fitting() | 0.11 | 0.101 |  | 0.03 | 0.101 | 
estimate |  | 0.62 | 0.71 |  | 0.65 | 0.67
fitting | 0.79 | 0.61 |  | 0.52 | 0.54 | 
 | 2020[11] (PPLN) | 2020[53] (PPLN) | 2019[1] (PPLN+DC) | 2018[4] (PPLN+3*DC) | 2016[12] (PPLN) | Our estimate (PPLN)
Squeezing Level(dB) | -6.3 | -4 | -2 | -1.38 | -1.83 | -0.67
Waveguide type | Ridgea | Ridgeb | SPE | RPE | Ridgec | Ti
QPM length(mm) | 45 | 45 | 30 | 20 | 40 | 15
 | 57.28 |  |  | 92.5 | 125 | 15.8
 | 0.108 |  |  | 0.061 | 0.141 | 0.019
 | 0.11 | 0.101 |  | 0.03 | 0.101 | 
 |  | 0.62 | 0.71 |  | 0.65 | 0.67
 | 0.79 | 0.61 |  | 0.52 | 0.54 | 
: SH conversion efficiency
: SH conversion efficiency root
: Total effective detection efficiency
aZnO:LN bonded onto LiTaO3 bLN bonded onto LiTaO3 cLN etching
SPE=soft-proton exchange RPE=reverse proton exchange
Different waveguide type and longer QPM length provide more nonlinear conversion efficiency
Ti-indiffused waveguide efficiency almost RPE waveguide 0.17 times
Notes: 再量測壓縮光可以分為兩個部分討論 第一種是晶片的非線性的轉換效率 其次是光路的偵測效率
這個表格主要是討論我們所設計的晶片所使用的波導材料以及具備的轉換效率 和其他文獻的差別 可以看到他們所使用的QPM長度大多是我們兩倍的長度，使用的材料效率最差的是SPE的波導 效率比鈦高

## Slide 46
Our measurement:
SH conversion efficiency 0.019)
η = 0.67
Estimate squeezing level at pump power = 40mW
Longer QPM length get more squeezing level
QPM length(mm) | 15 | 30 | 38 | 45
Squeezing Level (dB) | -0.67 | -1.28 | -1.58 | -1.83
Calculation squeezing level
Efficiency factor | parameter | value
LN-air interface | ηF | 0.86
Free space transmission | ηf | 0.985
PD quantum efficiency | ηPD | 0.995
PD electronic noise | ηe | 0.98
Mode match(visibility) | ηvis | 0.9
Total detection efficiency | η | 0.67
η = ηF · ηf · ηPD ·ηe ·
Notes: 所計算的方式是使用

## Slide 47
Introduction
Theory
Simulation
Fabrication process
Experimental Results and Analysis
Conclusion and future work

## Slide 48
We demonstrated :
Successfully fabricated the periodically poled lithium niobite(PPLN) cascaded adiabatic beam splitter on chip.
PPLN normalize second harmonic generation efficiency 15.8%/W/cm2 with 15mm QPM length.
Adiabatic coupler as beam splitter which the characteristic ER>10dB with 68nm bandwidth, ER>20dB with 18nm bandwidth and coupling ratio up to 99.5% at 1550nm.
Optimized on-chip squeezer measurement setup, including 775nm pump wavelength coupling efficiency in waveguide, mode matching.
775nm coupling efficiency improved by fiber coupling, from -8.5dB to-4.8dB.
Mode matching via fiber mode() replaced by waveguide mode().
Conclusion

## Slide 49
Future work
On-chip squeezer enhance:
The adiabatic beam splitter component require longer coupling length. That is, reducing nonlinear conversion efficiency so that limit the squeezing level.
Longer QPM length.
Change waveguide type.
Squeezing setup stabilize:
Achromatic objective lens
Chip oven temperature control system
Notes: 先不使用AC做分光 先將QPM長度拉長提高非線性效率
希望整合更多元件就會建議採用其他種類的波導
架構已經完整了，可以加消色差物鏡耦合方式、設計更為穩定的溫控器，使得量測系統更加完善穩定

## Slide 50: Thank you for listening !

## Slide 51
正比L
正比
Photorefractive effect
本論文選擇此溫度為操作溫度的原因是為了消除光折變效應(photorefractive effect)，其原理為當一強光集中於特定區域，像是本論文中的波導結構時，會激發出晶體中的電子，但此電子會被侷限住形成不均勻的電場，此電場會因為晶體本身是鐵電性晶體的關係而造成折射率的改變，影響到原本計算出來的非週期性晶疇極化反轉結構，降低非線性轉換的效率，當溫度越高時，電子變越不容易被侷限在特定區域，如此便可以減低光折變效應所帶來的影響。
Gain-induced diffraction
在high gain狀況下，signal容易被pump影響，會讓squeezed beam產生相位的破壞，且空間上不會合LO beam match，所以LO無法準確的偵測squeezed quadrature

## Slide 52
High-pass filter simulation

## Slide 53
High-pass filter simulation

## Slide 54
Propagation loss scheme

## Slide 55
Propagation loss
鈦擴散波導(左)TM偏振傳播損耗、 (右)TE偏振傳播損耗
，

## Slide 56
ER spectrum
Notes: ER>10dB with 50nm

## Slide 57
Calculation squeezing level
 | 2020[11] (PPLN) | 2020[53] (PPLN) | 2019[1] (PPLN+DC) | 2018[4] (PPLN+3*DC) | 2016[12] (PPLN) | Our estimate (PPLN)
Squeezing Level(dB) | -6.3 | -4 | -2 | -1.38 | -1.83 | -0.67
Waveguide type | Ridgea | Ridgeb | SPE | RPE | Ridgec | Ti
QPM length(mm) | 45 | 45 | 30 | 20 | 40 | 15
norm(%/W/cm2) | 57.28 |  |  | 92.5 | 125 | 15.8
) | 0.108 |  |  | 0.061 | 0.141 | 0.019
fitting() | 0.11 | 0.101 |  | 0.03 | 0.101 | 
estimate |  | 0.62 | 0.71 |  | 0.65 | 0.67
fitting | 0.79 | 0.61 |  | 0.52 | 0.54 | 
SPDC conversion efficiencies (pairs/mW/GHz/s) |  |  | ~105 |  | ∼1.2 · 106 | 
Propagation loss(dB∕cm) |  |  | 0.04 | 0.14 | 0.4 | 0.2
 | 2020[11] (PPLN) | 2020[53] (PPLN) | 2019[1] (PPLN+DC) | 2018[4] (PPLN+3*DC) | 2016[12] (PPLN) | Our estimate (PPLN)
Squeezing Level(dB) | -6.3 | -4 | -2 | -1.38 | -1.83 | -0.67
Waveguide type | Ridgea | Ridgeb | SPE | RPE | Ridgec | Ti
QPM length(mm) | 45 | 45 | 30 | 20 | 40 | 15
 | 57.28 |  |  | 92.5 | 125 | 15.8
 | 0.108 |  |  | 0.061 | 0.141 | 0.019
 | 0.11 | 0.101 |  | 0.03 | 0.101 | 
 |  | 0.62 | 0.71 |  | 0.65 | 0.67
 | 0.79 | 0.61 |  | 0.52 | 0.54 | 
SPDC conversion efficiencies (pairs/mW/GHz/s) |  |  | ~105 |  | ∼1.2 · 106 | 
Propagation loss(dB∕cm) |  |  | 0.04 | 0.14 | 0.4 | 0.2
SH conversion efficiency :(%/), Normalize (%// cm2)
SH conversion efficiency root :
Total effective detection efficiency :
aZnO:LN bonded onto LiTaO3 bLN bonded onto LiTaO3 cLN etching
SPE=soft-proton exchange RPE=reverse proton exchange
Notes: 再量測壓縮光可以分為兩個部分討論 第一種是晶片的非線性的轉換效率 其次是光路的偵測效率
這個表格主要是討論我們所設計的晶片所使用的波導材料以及具備的轉換效率 和其他文獻的差別 可以看到他們所使用的QPM長度大多是我們兩倍的長度，使用的材料效率最差的是SPE的波導 效率比鈦高